Resin used: Siraya Tech Sculpt High-temperature resistant resin in clear color.

Printer used: Elegoo Mars 3 Pro with a magnetic removable build plate.

Print settings:

Post processing steps:

- Spray with acetone

- Blow dry with compressed high pressure nitrogen

- Repeat steps 1-2 until pins are completely clean of residual resin (6-8 cycles)

- Remove flexible metal plate from printer build plate.

- Place inside Elegoo Mercury X rotating UV cure station.

- UV cure for 15 minutes.